Fusion 360 Slicing Tips

- Create a new Print setting (copy it from one you already have) and save it to your Cloud

  - This will enable you to access it anywhere

- Edit the Manufacturing Model to ensure you are only printing what you want to print

- If prints are stringy, try:

  - Reducing extrusion temperature

  - Increasing retract length

- If prints are too weak

  - Increase infill percentage

  - Increase shell thickness (more layers on perimeter, top, & bottom)

- If parts fail without support

  - Try reorienting the part

  - Try adding supports (ensure to add them where they will be easy to remove)

- If prints do not stick on the first layer

  - Check bed temperature

  - Check bed leveling

  - Try different Print Bed Adhesion settings (listed in order of strength)

    - Skirt is a thin ring around, but no connected to, the part(s)

    - Brim is a thin plate under the part(s)

    - Raft is a thick plate under the part(s)

- Remove the blob at the end of a print by reducing the final extrusion setting in the last G1 move

- Modify final lines of gcode to make printing faster